## Slide 1
The effects of Annealing the Mechanical Properties on Additive Manufactured Thermoplastics
Juan Lopez, Travis Welch, Philip Velbis, Jose Reyna
Background and Objective: 3D printed objects when printed have weak layer bonds. The reason that the bonds might be weak is due to little air gaps in between the plastic. The goal is to heat the object to release the air gaps to lessen the internal stress to increase the strength.
Acknowledgments:
This project is supported by the US Department of Education through the through the Minority Science and Engineering Improvement Program (MSEIP, Award No. P120A150014); and through the Hispanic-Serving Institution Science, Technology, Engineering, and Mathematics (HSI STEM) Program, Award No. P031C110159.
Process:
This image shows what we hope to accomplish with treating our material with heat from the surface, where the air gaps are going away allowing recrystallization
Before:
After:
When something is being printed using Fused Deposition Modeling (FDM) there will always be a little bit of space somewhere in between them due to material being stacked on each other.
Printing:
We printed our parts going upwards rather than laying flat on the print bed. The layers on the flat print go lengthwise rather than side to side. We want to test the layer bond not the plastic itself
Approach:
Results:
We were looking for a few things from the tests
The raw data
How the specimen broke
The Graphs
Data Calculations
Annealing:
We had a total of 9 batches consisting of 3 specimen each
We annealed at 4 different temperatures and at 4 different times
We used a Quincy Labs Model GC oven
For our testing we chose the ASTM d638 type 1(American Society for Testing and Materials), which is the best type for tensile testing plastics
From there we had to create the specimen in Solidworks where we had to design something wouldn’t fall over
We used Cura to be able to able to go from Solidworks to a 3D printer. Within Cura we had a slot of settings to configure for the best print
14 hours per print
5 different printing designs
1/3 failed
We started with placing the specimen on metal plates but they seemed to warp consistently so we switched to a glass plate where there was less warping
Tensile Testing:
We ran the specimen at .05mm/s for the first batch
We ran .01mm/s for the rest of the batches
Batch | Time(min) | Temperature(°C) | Avg Toungness (J/m^3) | Avg E(N/m^2)
1 | None | None | 4.22465 | 9.0256
2 | 60 min | 60 | 12.4207 | 5.87675
3 | 60 min | 75 | 4.142167 | 7.164167
4 | 60 min | 90 | 3.375067 | 15.546
5 | 60 min | 80 | 4.005467 | 7.611133
6 | 60 min | None | 116.8257 | 6.664733
7 | 90 min | 60 | 4.549633 | 8.9444
8 | 120 min | 60 | 4.3722 | 8.822967
9 | 30 min | 60 | 12.94667 | 6.460667
From the graphs we were able to find the Toughness, Elastic Modulus, Yield Strength, Ultimate Strength, Fracture Strength, and Resilience.
There are different types of breaking, and there is also necking
Most of our samples looked brittle when they broke, but a few seemed more ductile after annealing
Chart: All Stress vs Strain Samples
| 0 | 2.2370000000000001E-2 | 7.2260000000000005E-2 | 0.1045 | 0.14101 | 0.17588000000000001 | 0.2114 | 0.24648999999999999 | 0.28114 | 0.31645000000000001 | 0.35197000000000001 | 0.38607000000000002 | 0.42193000000000003 | 0.45690999999999998 | 0.49199999999999999 | 0.52685999999999999 | 0.56272 | 0.59682000000000002 | 0.63212999999999997 | 0.66798000000000002 | 0.70196999999999998 | 0.73728000000000005 | 0.77292000000000005 | 0.80757000000000001 | 0.84265000000000001 | 0.87839999999999996 | 0.91249999999999998 | 0.94835999999999998 | 0.98333000000000004 | 1.01831 | 1.0533999999999999 | 1.05921
 | -0.00337 | 0.10401 | 0.67168 | 1.0149 | 1.397 | 1.7584 | 2.1224 | 2.4879 | 2.8373 | 3.1504 | 3.505 | 3.8371 | 4.1814 | 4.5215 | 4.8584 | 5.1973 | 5.5256 | 5.8517 | 6.1821 | 6.5087 | 6.815 | 7.1474 | 7.4648 | 7.7848 | 8.0931 | 8.4115 | 8.714 | 9.0204 | 9.3227 | 9.6187 | 9.6662 | 5.5874
 | -0.39782 | -0.36628 | -0.08286 | 0.10534 | 0.29165 | 0.48078 | 0.66671 | 0.83946 | 1.0097 | 1.1836 | 1.3563 | 1.5312 | 1.7042 | 1.8792 | 2.0511 | 2.2197 | 2.3894 | 2.5642 | 2.7432 | 2.9095 | 3.0727 | 3.2367 | 3.4052 | 3.5732 | 3.7386 | 3.9043 | 4.0679 | 4.2292 | 4.4048 | 4.5618 | 4.7279 | 4.8902 | 5.053 | 5.2054 | 5.3686 | 5.5291 | 5.6876 | 5.8515 | 6.0053 | 6.159 | 6.3167 | 6.4753 | 6.6269 | 6.7878 | 6.9439 | 7.0907 | 7.2382 | 7.3928 | 0.64309
 | 0.01474 | 0.18092 | 0.91698 | 1.3713 | 1.9135 | 2.4117 | 2.9089 | 3.4 | 3.8781 | 4.3733 | 4.8659 | 5.3556 | 5.8412 | 6.3254 | 6.787 | 7.2587 | 7.7378 | 8.2105 | 8.6746 | 9.1438 | 9.6017 | 10.0599 | 10.5121 | 10.9487 | 11.3857 | 11.8296 | 12.2472 | 12.6782 | 13.1012 | 13.48 | 13.8644 | 14.229 | 14.5668 | 8.2257
 | 0.00125 | 0.13332 | 0.89328 | 1.316 | 1.8421 | 2.3222 | 2.8104 | 3.2805 | 3.7367 | 4.2084 | 4.6785 | 5.1429 | 5.5984 | 6.0577 | 6.5012 | 6.9529 | 7.401 | 7.8489 | 8.2804 | 8.7095 | 8.5447 | 8.7029 | 8.2223 | 0.95257
 | -0.00366 | 0.06703 | 0.4106 | 0.62288 | 0.89984 | 1.1443 | 1.4215 | 1.6936 | 1.9879 | 2.2861 | 2.589 | 2.8953 | 3.2169 | 3.5408 | 3.8768 | 4.2217 | 4.577 | 4.928 | 5.292 | 5.6627 | 6.0239 | 6.3984 | 6.7871 | 7.1685 | 7.5552 | 7.9475 | 8.3294 | 8.7111 | 9.0921 | 9.442 | 9.781 | 0.95772
Conclusion:
Annealing a 3D printed object can help the mechanical properties including toughness, Elastic modulus, Yield Strength, Ultimate Strength, Fracture Strength, and Resilience
Annealing PLA at a lower temperature helps the toughness rather than high heat
Specimen were less brittle and more ductile